## Slide 1
Volumetric strain measurements in the D-DIA for probing transformation plasticity and semi-brittle deformation
Lars Hansen (UMN), Andrew Cross (WHOI), David Goldsby (UPenn), and Adaire Nehring (UMN)
With additional contributions from:
Tom Breithaupt, Haiyan Chen, Amanda Dillman, David Goldsby, Rellie Goddard, Diede Hein, Katie Kumamoto, Veronique Le Roux, Caroline Seyler, Chris Thom, David Wallis

## Slide 2
Constant twist rate
α-Fe
γ-Fe
α-Fe
γ-Fe
Hot
Cold
Cold
Sauveur (1924)
Iron bars in torsion
PART 1:
Transformation plasticity as a deformation mechanism
Notes: Comparatively few experiments on phase transitions – but interest in the topic goes back almost 100 years

## Slide 3
Shear zone nucleation during orogenesis (Schmidt et al., 2003)
Decoupling of mantle convection (Parmentier, 1981; Rubie & Brearley, 1984)
Slab stagnation in mantle transition zone (Sammis & Dein, 1974; Panasyuk & Hager, 1998)
Seismic uncoupling along subduction interfaces (Ruff & Kanamori, 1981)
Deep focus seismicity (Bridgman, 1945; Green & Burnley, 1989)
Mantle plume dynamics (Gordon, 1971)

## Slide 4: Greenwood & Johnson (1965) model
Strain
Stress
1) applied stress < yield stress
2) volume change introduces internal stress
3) plastic flow produces permanent strain
Notes: G&J model introduces concept of internal stress – produces anomalous weakening

## Slide 5
Hydrostatic
(σ1 = σ2 = σ3)
Non-hydrostatic
(σ1 > σ2 ≥ σ3)
σ1
σ2
σ3
Notes: And also predicts volume change anisotropy

## Slide 6: Conventional rigs not well suited to studying transient phenomena
Griggs apparatus
Paterson apparatus
Thick steel pressure vessel
P < 2 GPa
P < 0.3 GPa

## Slide 7
linear
accelerator
booster synchrotron
storage ring
X-rays
Utilizing the D-DIA at 6-BM-B at the Advanced Photon Source

## Slide 8
sample
D-DIA assembly and apparatus

## Slide 9: Energy Dispersive X-ray diffraction provides in-situ stress…
(002)
(130)
(112)
(131)
(041)
(210)
(122)
(140)
(211)
2.8
3.0
2.6
2.4
2.2
2.0
Lattice spacing, d (Å)
1
2
3
4
5
6
7
8
9
10
Intensity
1
2
3
4
5
6
7
8
9
10
X-rays
detector
array
after Goddard et al. (submitted)

## Slide 10
Quartz
Olivine
opaque WC anvil
0.5 mm
Al2O3 piston
Al2O3 piston
…strain resolution down to 10-5…
Notes: Detect changes in length down to one hundredth of a percent

## Slide 11
Quartz
Olivine
opaque WC anvil
0.5 mm
Al2O3 piston
Al2O3 piston
…strain resolution down to 10-5…
axial displ.
radial displ.
Notes: Detect changes in length down to one hundredth of a percent

## Slide 12
P
(GPa)
Transform quartz into coesite (and back to quartz) under:
Hydrostatic conditions (no deformation)
Non-hydrostatic conditions (during creep deformation)
Experiments
1)
2)

## Slide 13
San588: quartz-coesite (SiO2) @ 900°C
Non-hydrostatic
Cross et al. (2025)

## Slide 14
Slow deformation
(0.0003 mm/s)
Fast deformation
(0.01 mm/s)
Viscosity
% coesite
Viscosity
Cross et al. (2025)
Significant viscosity reduction depending on relative rates of deformation and transformation
Notes: Up to two orders of magnitude weakening during the phase transformation.
Magnitude of transient weakening doesn’t appear to be temperature sensitive. However, it *is* rate sensitive – basically, it’s all controlled by the rate of deformation versus the rate of transformation. When the transformation is fast, relative to deformation (left hand panels), there’s marked weakening. On the other hand, when deformation is fast relative to the transformation, there’s little weakening.
Maybe this is all controlled by the relative proportions of transformation and deformation related dislocations?

## Slide 15
PART 2:
Elucidating the micromechanics of semibrittle flow
Wen et al. (Comp. Geo., 2022)
crack nucleation, growth, interaction
dislocation-crack interactions
dislocation interactions

## Slide 16
Built on the work of:
Sibson, 1977
Bird, 1978
Goetze and Evans, 1979
Brace and Kohlstedt, 1980
Kirby, 1980
Kohlstedt, Evans and Mackwell 1995
Mei et al., JGR, 2010
Semibrittle flow is the poorest constrained aspect of lithospheric strength

## Slide 17
Strain
Stress
Progressive activation of different mechanisms

## Slide 18
Strain
Stress
Progressive activation of different mechanisms
dislocation nucleation and glide

## Slide 19
Strain
Stress
Progressive activation of different mechanisms
dislocation interactions and backstress

## Slide 20
Strain
Stress
Progressive activation of different mechanisms
crack nucleation and growth

## Slide 21
Strain
Stress
Progressive activation of different mechanisms
Brantut (2025)
steady-state semibrittle flow?
dislocation-crack interaction

## Slide 22
opaque WC anvil
0.5 mm
Al2O3 piston
Al2O3 piston
coarse
fine
Experiments on semibrittle flow of olivine
Notes: Detect changes in length down to one hundredth of a percent

## Slide 23
Nehring et al. (in prep.)
Room temperature
Range of behaviors depending on pressure

## Slide 24
Nehring et al. (in prep.)
Room temperature
brittle failure
Room temperature
Range of behaviors depending on pressure

## Slide 25
Nehring et al. (in prep.)
Room temperature
semi-brittle flow?
Room temperature
Range of behaviors depending on pressure

## Slide 26
Nehring et al. (in prep.)
Are cracks produced during deformation or unloading?

## Slide 27
Dilation measured during deformation
↑ compaction
↓ dilation

## Slide 28
Dilation measured during deformation

## Slide 29
room temperature
8 10

## Slide 30
8 10
Brantut (2025)
room temperature

## Slide 31
Nehring et al. (in prep.)
Brantut (2025)
Best-fit of this model to our data

## Slide 32
Previous best guess w/out semi-brittle flow
Incorporation of semi-brittle flow
Nehring et al. (in prep.)
Extrapolation to the lithosphere—major strength reduction