## Slide 1: High Speed X-ray Imaging at High Pressure and Temperature
Eglantine Boulard
Sorbonne Université, IMPMC
Soleil Synchrotron
N. Guignot, A. King, J-P Deslandes & J-P Itié (Soleil Synchrotron)
J-P Perrillat ; P. Garcia del Real; E. Giovenco (Lyon University)
Y. Le Godec (IMPMC)
A. Dewaele & C. Denoual (CEA)

## Slide 2
The French national synchrotron radiation source
Located at St Aubin, 25 km south of Paris
First electrons accelerated in 2006
2.75 GeV storage ring, 354 m circumference
450 - 500 mA top up
29 beamlines, 3 tomography beamlines:
  PSICHE
  ANATOMIX – dedicated imaging beamline
  PUMA – dedicated to cultural heritage and ancient materials

## Slide 3: Psiché Beamline
Pression, Structure et Imagerie par Contraste à Haute Energie
Highest energy beam line at SOLEIL
Diffraction at extreme pressures:
  Diamond anvil Cells, Paris-Edinburgh, Multi-anvil
  Monochromatic / angular dispersive XRD
  White beam / energy dispersive XRD (CAESAR)
Tomography
  Polyvalent and flexible
  Combine techniques

## Slide 4
D1
LVP
DCM
VFM
Tomo
C
D2
DAC
Experimental hutch
Optics hutch
CAESAR
KB
slits
Primary slits
or
Multi-anvil press
Paris-Edinbourgh press
Table 3
Table 2
Table 1
shutter
26 m from Wiggler souce
31 m from Wiggler souce
37 m from Wiggler souce
F

## Slide 5: Tomography at Psiché
Designed for material science
Fast: <5 seconds/scan
High resolution: 0.5 μm (0.127 μm pixels)
High energy: >80keV pink beam
Monochromatic range
Pink beam range…
Notes: In situ experiments : Stress rig
Can go fast : "video" Al Cu, cristallisation
High resolution: dist + phase contrast

## Slide 6
H. Coqueugnoit et al (Bordeaux)
S. Delzon et al (INRA)
high precision - high load - large aperture
Large and/or heavy samples (up to 50 Kg) and in-situ setups
Rotation Stage
Notes: high load,large samples = important for being able to do it in a LVP

## Slide 7: Radiography in Multi-Anvil Press
Alignment tool for diffraction
Primary diagnostic: falling sphere viscosity measurements
High speed pco.dimax camera from ANATOMIX beamline
(KHz frame rate)
As measured
Background corrected
A. Yoneda, Okeyama University, SOLEIL proposal 20160333

## Slide 8: Paris-Edinburgh Press
Jouini et al., J. Superhard Mater, 2016
Klotz et al., Applied Physics Letters, 2005

## Slide 9
Philippe et al. 2016
RoToPEC
A. Clark et al.
Pros : High quality images
Cons: necessitates long acquisition time (20 min)
Tomography Through Paris-Edinburgh Press

## Slide 10: High-Speed Tomography at HPHT: ~10s
Boulard et al., JSR, 2018
4 columns PE Press (135 ° opening, P constant )+ Pink Beam

## Slide 11: High-Speed Tomography at HPHT
Powdered Rhyolite + Olivine Cristals
Image liquids
Vesiculation/Cristalization rate
Diffusion Profile

## Slide 12: Ex#1: Liquid Carbonate Percolation
Naif et al., 2013
Hammouda & Laporte 2000
High mobility of carbonate liquids:
Dasgupta & Hirschmann 2010

## Slide 13: Ex#1 : Liquid Carbonate Percolation
olivine
carbonate
olivine
J-P Perrillat
P. Garcia del Real
E. Giovenco
650 µm
1.7 GPa – 1150 K
650 µm

## Slide 14
olivine
carbonate
olivine
650 µm
J-P Perrillat
P. Garcia del Real
E. Giovenco
Ex#1 : Liquid Carbonate Percolation
1.7 GPa – 1150 K
650 µm
1.7 GPa – 1300 K
650 µm

## Slide 15: Ex#1 : Liquid Carbonate Percolation
1.7 GPa – 1150 K
olivine
carbonate
olivine
650 µm
650 µm
1.7 GPa – 1300 K
650 µm
Distance in m2
Diffusion Profiles:
Diffusion coefficient : 6.5 10-11 m2/s at 1300 K
J-P Perrillat
P. Garcia del Real
E. Giovenco

## Slide 16: Modified PE Press: UToPEC <10s
165° opening
170 mm ⌀
﻿rotary coupling

## Slide 17: Ex#2: In Situ Analyses of Microstructures in the α-γ-ϵ Fe Phase Transitions
Possibility to collect simultaneously XRD and Tomography:
XRD: CAESAR detector
Tomography
Dewaele
Y. Le Godec (IMPMC)

## Slide 18: Ex#2: In Situ Analyses of Microstructures in the α-γ-ϵ Fe Phase Transitions
Dewaele et al., ﻿Appl. Phys. Lett., 2018
Mechanisms involved in phase transitions:
Orientation Relationship
Interface/habit planes between phases
﻿CrMnNi cast steel
Ackermann, metal. Mater. Trans. a., 2016

## Slide 19: Ex#2: Material & Method
Single cristal of Iron
001 oriented
Rz: rotation angle/Xrays
XRD analyses : orientation of the single cristal
Upon phase transition : XRD + Tomography analyses
    orientation relationship + microstructures

## Slide 20: Ex#2: α-γ Fe Phase Transition
γ grows as few large single crystals with different orientations
{011}α // {111}γ planes
Boulard et al., in prep.
Transformation paths:
~2 Gpa - 1000 K :
α
γ
Nishiyama–Wasserman
Kurdjumow - Sachs

## Slide 21: Ex#2: α-γ Fe Phase Transition
α-Fe and γ-Fe phases can be detected by absorption contrast (density difference ~2.2%)
The α-Fe and γ-Fe interface approximately follows an isotherm
suggest a mechanism with a relatively low energy cost
Interface ~ parallel with (110)α (expected) or (310)α planes (not expected)
Boulard et al., in prep.
~5 Gpa – 900 K
~2 Gpa - 1000 K

## Slide 22: Ex#2: γ- ϵ Fe Phase Transition
γ-Fe ϵ-Fe phases hardly detectable by absorption contrast
The γ-ϵ interface irregular
~8 Gpa - 800 K :

## Slide 23: Ex#2: α-ϵ Fe Phase Transition
α-Fe grows as thin plates, multiple orientations
(multiple grains of ϵ-Fe )
Boulard et al., in prep.
~8 GPa - 725 K
~6 GPa – 680 K

## Slide 24: Ex#2: α-ϵ Fe Phase Transition
Chcp-ϵ axis parallel to the two (110)α
as expected by Burgers mechanism
Dewaele et al., ﻿PRB, 2015
Boulard et al., in prep.
~10 Gpa - 700 K :

## Slide 25: Ex#2: α-ϵ Fe Phase Transition
ϵ-Fe grows as thin plates bursting everywhere in the sample
Eventually, the space between the plates also transforms to ϵ-Fe
The size of these domains adapts to the size of the sample
Boulard et al., in prep.
~10.6 GPa - 800 K
time

## Slide 26
Ex#2: α-ϵ Fe Phase Transition
3D Fourier transform calculated for a tomography
maxima correspond, within 5°, to the directions of (112)α planes
expected habit planes for Burgers paths
Orientation of ϵ-Fe plates:
Boulard et al., in prep.

## Slide 27: Conclusions
By combining :
Adapted tomograph stage (high load, high speed, high precision)
Fast detectors
Pink Beam
Fast processes
Liquids behavior
Reactions/Crystallisation/Vesiculation rates
Phase Transition mechanisms
we collected tomography “continuous” scans in ~10s at HP-HT
New PE press (UToPEC) :
increase the quality of the images (smaller, wider opening)
perform scans <10s (rotary coupling)

## Slide 28: Aknowledgments
Andrew King
Nicolas Guignot
Jean-Pierre Deslandes
Jean-Paul Itié
Jean-Philippe Perrillat
Pablo Garcià Del Real
Elena Giovenco
Yann Le Godec
Alisha Clark
Guillaume Morard
INSU PNP - 2017
DIM OxyMORE, île de France Region - 2016