## Slide 1: The LVP beamline P61B at PETRA III:
Development and experiments
Robert FARLA
APS, Argonne Nat. Lab, USA 28 September 2018
Ack: Shrikant Bhat, Stefan Sonntag, Nico Gaida, Eleonora Kulik, Norimasa Nishiyama, Wolfgang Drube, Tomo Katsura

## Slide 2: Overview of P61B (PETRA III)
01 Strategy of operation
02 Beamline characteristics
03 High-pressure techniques
04 Science highlights (ex situ studies)
05 Instrumentation (detectors…)
06 User support
07 Future plans (supply/demand)
08 Summary

## Slide 3: Strategy for beamline operations
Serving the Earth and Materials Science communities
I. Geochemistry, Geophysics, Seismology,…
The Earth
Phase relations: • Transformation • Nucleation • Melting curves (solidus/liquidus) • Equations of state
Controlled rock deformation
Melt viscosity measurements
Amorphous materials
Acoustic interferometry
Electrical conductivity

## Slide 4: Strategy for beamline operations
Serving the Earth and Materials Science communities
II. Materials Science: functional materials with exotic properties
Phase relations: • Transformation • Nucleation • Melting curves (solidus/liquidus) • Equations of state
Characterization of new unknown structures
Large (~1 cm3) sample synthesis • Hardness testing, etc.
Band-gap tuning / semiconductors
Super-hard
Optical windows
Super-conductive
Sn-Ge-Si, Ta & Ga Nitrides
Tellurides (CrTe3)
Indium oxides (In2O3)
Si-Ti-C nitrides
Metal borides
Carbides
cubic-Si3N4
Al2SiO5 kyanite / Al2O3 / SiO2 nano-composites
Metal hydrides
Quadruple perovskites (AA′3 B4O12)
Catalyzers
Numerous uses in industry, multi-billion dollar markets

## Slide 5: Beamline construction
10 Jan 2018

## Slide 6: Beamline construction
Control hutch + XRD lab
XRD lab and CNC room (behind)
Beam transport tunnel (to P61B)
View inside tunnel
Today

## Slide 7: Beamline characteristics
10x Wigglers
Detector table
P61B LVP
P61A HZG
Absorber
(50%)
(50%)
Hall North (140 m)
Source: 10 Wigglers
Energy range: 30-200 keV
Flux: ~1011 – 1012 ph/s
Max. beam size (mm2): 1.5x1.5
Distance from last wiggler:
133 m
First beam:
expected early 2019
EH LVP
OH LVP
CH LVP
EH HZG
CH HZG
1 x 1 mm2
2 mm (v)
x 3 (h) mm
Front End

## Slide 8: Beamline characteristics
Source: 10 Wigglers
Energy range: 30-200 keV
Flux: ~1011 – 1012 ph/s
Max. beam size (mm2): 1.5x1.5
Power density: 12 W/mm2 (1x CVD+Cu filter) 9 W/mm2 (3x CVD+Cu filters) 7 W/mm2 (3x CVD+Cu,1xC)
Flux for 1 mm2 beam
10 wigglers in the ~100 m straight section

## Slide 9: High-pressure techniques
Diffracted
X-rays
Anvil TEL
OCT
Sample ø
1 - 3 mm
1 mm
6-8 geometry
14/7 assembly
1200 ± 30 °C
200 °C
Power = 720 W
Compression geometry
Assembly & heating
60 GPa
Diffracted
X-rays
2nd
Sample ø
6 mm
6-6 geometry
20/15 assembly
Power = 740 W
1200 ± 30 °C
100 °C
2 mm
2
Large chamber between 6 rams to accommodate various multi-stage set ups
Numerical simulations using CellAssembly (Hernlund et al. 2006)
ZrO2
LaCrO3
MgO
Mo
WC
ZrO2
MgO
Cu
graphite
pyrophyllite
WC

## Slide 10: ‘Kawai’ octahedral geometry (6-8)
Before compression
After compression
ZnTe 
ZnTe 
ZnS 
GaAs 
GaP 
Room temperature
Sample sizes:
8/3 ~ 1 mm
10/4 ~ 1.5 mm
14/7 ~ 2 mm
18/10 ~ 2.5 mm
Isotropic compression

## Slide 11: ‘Kawai’ octahedral geometry (6-8)
Targeting pressures > 40 GPa at high temperatures in the LVP
Spacer system with cage to shrink 1st stage anvil EL from 60 mm to 50 mm for smaller WC anvils (27 mm EL).
Fujilloy F05 anvils with negative tapers (-1°)

## Slide 12: Cubic geometry (6-6)
Chart: Load (MN)
| 38.095238095238102 | 380.95238095238102 | 761.90476190476204 | 1142.8571428571431 | 1523.8095238095241 | 1904.761904761905 | 2285.7142857142862 | 2666.666666666667 | 3047.6190476190482 | 3428.5714285714294 | 3809.5238095238101 | 4190.4761904761908 | 4571.4285714285725 | 4952.3809523809532 | 5333.3333333333339 | 5714.2857142857156 | 6095.2380952380963 | 6476.1904761904771 | 6857.1428571428587 | 7238.0952380952394 | 7619.0476190476202 | 8000.0000000000018 | 8380.9523809523816 | 8761.9047619047633 | 9142.8571428571449 | 9523.8095238095248 | 9904.7619047619064 | 10285.714285714288 | 10666.666666666668 | 11047.61904761905 | 11428.571428571431 | 11809.523809523811 | 12190.476190476193 | 12571.428571428574 | 12952.380952380954 | 13333.333333333336 | 13714.285714285717 | 14095.238095238097 | 14476.190476190479 | 14857.142857142861 | 15238.09523809524 | 15619.047619047622 | 16000.000000000004 | 16380.952380952383 | 16761.904761904763 | 17142.857142857145 | 17523.809523809527 | 17904.761904761908 | 18285.71428571429 | 18666.666666666672 | 19047.61904761905 | 19428.571428571431 | 19809.523809523813 | 20190.476190476194 | 20571.428571428576 | 20952.380952380958 | 21333.333333333336 | 21714.285714285717 | 22095.238095238099 | 22476.190476190481 | 22857.142857142862 | 23238.095238095244 | 23619.047619047622 | 24000.000000000004
BGI 8/6 fired | 0.23678 | 2.2389 | 4.1916 | 5.858 | 7.2381 | 8.332 | 9.1395 | 9.6608 | 9.8958
DESY 20/15 | 0 | 2.55 | 3 | 4 | 5 | 5.5 | 6 | 7
5/3 Co-MgO | 0 | 12 | 15.6 | 17.4
20/15 ~ 6 mm
Isotropic compression of very large sample volumes
30/20 ~ 10 mm
Mo
ZrO2
Mo (disc)
MgO
MgO/hBN
graphite
WC Anvils may not survive up to 15 MN…
50 mm ø base!
Pyrophyllite cube
(pre-fired @ 500 °C overnight)
Sample sizes:

## Slide 13: Cubic geometry (6-6)
6 mm
9 mm
12 mm
8/6 ~ 2 mm
5/3 ~ 1 mm
12 GPa
8/6
12/9
8 GPa
> 5 GPa
16/12
Kawazoe et al. 2010,2016
Manthilake et al. 2008
18+ GPa
15+ GPa
To do
 Bi III-V 
 ZnTe 
 ZnS
Room temperature
 ZnTe 
Sample sizes:
16/12 ~ 5 mm
12/9 ~ 3 mm
5/3
4/2.5
 Bi I-II-III
Load limit for WC 7% Co anvils with 25 mm ø
Pressure calibrations for “smaller” sample volumes at higher pressures

## Slide 14: Cubic geometry (6-6)
6
5
3
4
1
2
Controlled displacement rate of rams: 3,4: -7.2 µm/min (move in)
5,6: +7.2 µm/min (move out)
1: holds pressure at 45 bar (profile)
2: follows position of ram 1
This is constant volume anisotropic compression. Is sample pressure constant??
Anisotropic compression (deformation)

## Slide 15: Beamline highlights (ex situ)
- Synthesis of transparent cubic silicon nitride
Synthesis conditions: P ≈ 15.6 GPa, T > 1500 °C
Nishiyama N, Ishikawa R, Ohfuji H, et al. Scientific Reports 7:44755 (2017)
Transparent cubic silicon nitride (c-Si3N4)
Attractive choices for creating optical windows with supreme durability.
- Synthesis of transparent kyanite
Gaida N, Nishiyama N, Masuno A, et al. J Am Ceram Soc 100:323-332 (2017)
Transparent cubic kyanite (Al2SiO5)

## Slide 16: Beamline highlights (ex situ)
Synthesis of Sn-Ge-N compounds (courtesy of Dr. Bhat)
Band-gap tuning semi-conductors for solar-energy conversion and light emitting diodes

## Slide 17: Beamline highlights (ex situ)
Synthesis of Sn-Ge-N compounds (courtesy of Dr. Bhat)
At 15.6 – 20 GPa and 800 – 1000 °C
At 20 GPa and > 1000 – 1500 °C
Measurements done at P02.1, the powder diffraction beamline

## Slide 18: Beamline highlights (ex situ)
Synthesis of Sn-Ge-N compounds (courtesy of Dr. Bhat)
At 15.6 GPa and 800 – 1000 °C
At > 20 GPa and > 1100 °C
Measurements done at P02.1, the powder diffraction beamline
2 theta (Cu, K )
- Sn3N4
GNR θ-θ Europe XRD
(600 W)
Measurement below
Range: 10 – 110°
Anode: Cu, k
Acquisition time: 2 hrs
Throughput: > 10 kcps

## Slide 19: Beamline highlights (ex situ)
Pinch-and-swell structures of deformed amphibolite in marble (R. Farla)
Natural observations
Naxos, Greece
(Virgo et al. Solid Earth 2018)
Side
view:
Marble
Marble
Amphibolite ~ 0.3 mm
sample
stack
3
4
Amphibolite
Top
view:
MgO
MgO
Sample
stack
5
6
Experimental observations
Undeformed
εstack ~50%, εstack ~6 x 10-5 s-1
εstack ~50%, εstack ~6 x 10-5 s-1
P ~ 1.5 GPa T ~ 700 °C
P ~ 1.5 GPa T ~ 500 °C
P ~ 2 GPa T ~ 750 °C
5 mm
5 mm
5 mm
2 mm
Viscous boundinage
Notes: For 700 C: Boudin wavelength is 1000 um (1 mm), and n_marble = 11, and m ~ 2.5, then n_amph ~ 8 to 9 (ductile behaviour)
For 500 C: Boudin wavelength is 280 um, and n_marble = 11, and m ~ 2 to 3, then n_amph > 100 (brittle behaviour)!

## Slide 20: Synchrotron X-rays for the LVP
First light in the Front End of P61 (21 Aug 2018)
2x Ge-detectors
sCMOS camera
(not shown)
Detector table
5-axis stage
Incident
X-rays and slits
Press hydraulics
2 HP Ge-detectors for ED-XRD measurements, sCMOS camera for radiography
X-ray transport tube with adjustable slits (W, 10 mm thick blades)
5-axis stage [x, y1, y2, z (± 100 mm), rotation (± 20°)]

## Slide 21: Measurement techniques
Energy-dispersive X-ray Diffraction using 2 Ge-SSD
Principle:
where
Bragg’s law;
Scanned variable (by ED detector)
Determined variable
Fixed (by collimator)
Gauge (sample) volume
(e.g. 50 µm)
incident slits
receiving
slits
http://pd.chem.ucl.ac.uk/
Anticipated features:
Fast acquisition (10s of seconds)
Choice of diffraction angles
High throughput:
> million cps at 50 keV > 700 kcps at 122 keV
Electrically cooled: no maintenance
Advantageous for studies on low Z & amorphous materials
Possible implementation of CAESAR data acquisition for combined AD/ED-XRD

## Slide 22: Detector table
Call for tender out
Table can move backwards to make room (1.7 m) for a smaller roll in – roll out instrument (e.g. Paris-Edinburgh press from P02.2)

## Slide 23: Detector-collimator-slit system
Horizontal scanning detector #1

## Slide 24: Detector-collimator-slit system
Horizontal and vertical scanning detector #2

## Slide 25: Detector positioning
Top view
At -5°H and 5°H
Side view
At 5°H and 5°V
Detector movements:
x,y,z translations,
z-axis rotation,
y-axis rotation (vert. detector only)
Angular res: ± 0.0001 °
For CAESAR:
Angle step size: 0.001°
Movement precision: < 5 µm
Minimum angles
Distance sample to first slit in collimator
Receiving cross-slits
(10 mm tungsten blades)

## Slide 26: Detector positioning
Isometric view
Both detectors at max. 10° in horizontal plane
Top view
Max. 10° in horizontal without press rotation
10°
Detector 1
Incident X-rays
Maximum angles
Energy-dispersive X-ray Diffraction using two Ge-SSD
10°
Adjustable slits

## Slide 27: Detector positioning
Isometric view
Both detectors at max. 10° in horizontal plane
Energy-dispersive X-ray Diffraction using two Ge-SSD
Maximum angles
23.5°
Adjustable slits
Top view
Max. 10° in horizontal without press rotation
10°
Detector 1
Incident X-rays

## Slide 28: Detector positioning
One horizontal detector at max. to 20° with press rotation (max. 11.5°)
20°
Incident X-rays
Isometric view
Both detectors at max. 10° in horizontal plane
Energy-dispersive X-ray Diffraction using two Ge-SSD
Maximum angles
23.5°
Adjustable slits
11.5°
Detector 1

## Slide 29: Imaging
X-ray radiography using a white-beam microscope with double objectives
(10x, 20x)
sCMOS camera PCO.edge 5.5 MP
Scintillator and objectives
Camera and detectors set up in measurement positions
Example: X-ray radiography images of falling Pt sphere (Kono et al. 2014)
100 fps @ 5.5 MP or
> 1600 fps @ 2560 x 128
> 1 GB/s!

## Slide 30: User support
User-friendly operations with laboratory support
High-precision (20 µm)
CNC milling machine
for assembly parts
manufacture
Benchtop X-ray diffractometer (600 W)
for ex situ sample analysis
PUK welder
for precision welding
Lathe
for assembly parts
manufacture
Plus:
Ovens (storage and vacuum)
Firing furnace
Stereoscope, sensitive balance, low-speed diamond saw, drill, etc.

## Slide 31: Future plans (with X-rays available)
Expansion possibilities
Angle-dispersive XRD capability
  Installation of a double crystal Laue monochromator and 2D detector.
2nd LVP (< 1.7 m wide)
  Paris-Edinburgh press (ECB beamline P02.2)
  (rotational) Drickamer press?
RDA
Yale Univ.
P-E press
(at P02.2, PETRA III)
Design of mono from P21.2
Energy selection (> 40 keV), high bandwidth,
uses benders for Si crystals.
Impedance analyser for electrical conductivity measurements
  In situ technique also available without X-ray beam.

## Slide 32: Summary
Maximize 6-ram LVP capability:
  Pressure-temperature generation (> 60 GPa) ( > 2000 K)
  Sample size - cell assembly optimization
  Deformation mode (anisotropic compression)
Provide standard assemblies for users
Offer flexible experiment and measurement set ups
Easy-to-use graphical user interfaces

## Slide 33: Closing statements
A high-energy, extreme conditions beamline to serve a large community worldwide
Website: http://tiny.cc/petra3p61
Beamtime scheduling:
  With beam: 50%, shared with P61A
  Without beam: 50%, also open to proposals
Commissioning: ~ 1st half of 2019 User runs: late 2019, early 2020? Thank you for listening!

## Slide 34
FARLA, Robert
FS-PEX
robert.farla@desy.de
+49-40-8998-4470

## Slide 35: High-pressure techniques
Upper
Mantle
Transition zone
Lower Mantle
WC-anvils
Why a 6-rams Large Volume Press (LVP)?
Large samples (1-10 mm) (vs DAC samples < 0.1 mm)
Polycrystalline materials (incl. grain boundaries) diffusion, deformation, nucleation, seismic cracking,…
Further testing/analysis (e.g. hardness testing,…)
Highest pressures for 6-ram and DIA-type LVP
Isotropic & anisotropic compression (controlled rock deformation)

## Slide 36: Measurement techniques
Press pre-rotated to max. 11.5 ° to position one detector at up to 20°
20°
Incident X-rays
Isometric view
Both detectors at max. 10° in horizontal plane
Energy-dispersive X-ray Diffraction using two Ge-SSD
Maximum angles
23.5°
Adjustable slits
MgO pressure marker
Sample compositions
23.70 GPa
23.38 GPa
Ishii et al. (Farla, Kulik, Bhat) Scientific Reports. 2018
Complete agreement of the post-
spinel transition with the 660-km
seismic discontinuity
Rw
Rw
Rw
Rw
Rw
2θ = 7.2°

## Slide 37
Stability of dense hydrous magnesium silicates: ‘alphabet phases’ & others
Relatively cold oceanic crust carries water into the Earth as OH in hydrous phases, transformed by pressure.
→ Extending pressure range of 6-ram LVP to 65+ GPa at DESY
Ohtani et al. Geophys. Res. Lett. 2014
CWS-DESY: Fate of water in the deep mantle
Conventional LVP
Phases:
A, super-hydrous B (suB) = C, D = F & G, E, H, … and 10 Å, egg, δ-ALOOH,…
MgO-SiO2-H2O system

## Slide 38: Published ex situ studies (since 2015)
1. Synthesis of transparent cubic silicon nitride
Nishiyama N, Ishikawa R, Ohfuji H, et al. Scientific Reports 7:44755 (2017)
2. Transparent polycrystalline nanoceramics consisting of triclinic Al2SiO5 kyanite and Al2O3 corundum
Gaida N, Nishiyama N, Masuno A, et al. J Am Ceram Soc 101:998-1003 (2017)
3. A Complete Solid Solution with Rutile-Type Structure in SiO2 – GeO2 System at 12 GPa and 1600 °C
Kulik E, Nishiyama N, Masuno A, et al. J Am Ceram Soc 98:4111-4116 (2015)
GeO2
SiO2
(Si0.3,Ge0.7)O2
(Si0.5,Ge0.5)O2
(Si0.8,Ge0.2)O2
(Si0.9,Ge0.1)O2

## Slide 39: Highlight (Dr. Bhat)
Crystalline ternary B-C-N, a superhard phase?
Predicted by theory
Good chemical stability and oxidation resistance
High-T stability
Commercially hugely attractive ($20 billion market)
Yeung et al. Annual Review of Materials Research (2016)

## Slide 40: Highlight (Dr. Bhat)
BC4N and BC2N compounds
Amorphous BC4N and BC2N compounds decompose into c-BN and diamond. Thus, B-C-N materials remain elusive.
New boron oxynitrides (BON) compounds, e.g. B6N4O3 were discovered with yet unknown properties.

## Slide 41: Highlight (Dr. Bhat)
Sn3N4 and Ge3N4 (1:1) recovered from 15.6 GPa, 1000 °C – no solid solution…

## Slide 42: Highlight (Dr. Bhat)
XRD: Sn3N4 recovered from 20 GPa, > 1100 °C – new phase formation!

## Slide 43
λ = 645 nm
d = 0.8 mm
12/17
Transparency of the nanoceramic
Highlight (Nico Gaida)

## Slide 44
Highlight (Eleonora Kulik)
Fracture-induced amorphization leading to tougher ceramics

## Slide 45: Micro-mechanical bending test
Highlight (Eleonora Kulik)
Micro-mechanical bending test
Bridgmanite (MgSiO3)
Vickers hardness ~ 17 Gpa
(versus stishovite (SiO2) at 30 Gpa)

## Slide 46
  Cook and look experiments => create the P-, T- conditions, quench the sample and hope it stays the same
  In Situ experiments => create P-, T- conditions and measure the properties directly
In Situ techniques
  Raman/Infrared, Fluorescence, Brillouin Scattering, Electrical conductivity, Acoustic Emissions testing…
  X-ray Diffraction and X-ray Spectroscopy (synchrotron)
    Powder diffraction => phase identification and structural analysis (Rietfeld), deformation…
    Single crystal diffraction => full crystal structure characterization
    Fluorescence spectroscopy => chemical composition
    Imaging (radiography, phase contrast, tomography)
+
Tools for investigating Geophysical and Geochemical Processes
From ex situ to in situ studies – an eye opener

## Slide 47: Example study: Dehydration of subduction zone minerals
From Zeolith to Greenshist, Blueshist and Eclogite facies
https://upload.wikimedia.org/wikipedia/en/d/d1/Metamorphic_pathway_of_pressure-temperature_conditions_in_subduction_zones.jpg
Dehydration reactions in the subducted lithosphere:
Cause melting and volcanism
Trigger Earthquakes
Impact mantle convection
How much water is carried down?
Which hydrous and nom. Anhydrous minerals?
aus Winter 2001
1012 kg/year
Notes: One way of looking at what happens in more complex system in a simplified way is to look at the .so called facies => regions of the P-T phase diagram for all rocks.

## Slide 48: High-pressure techniques
Pressure media Heaters Refractory filling materials
Sample capsule
Pt, Re, Mo, Ni, Ta
Sample
10 mm
(Cr-MgO)
14 mm
(Cr-MgO)
18 mm
(Cr-MgO)
25 mm
(Co-MgO)
20 mm
Al2Si4O10(OH)2
Preformed
gaskets
Al2Si4O10(OH)2
LaCrO3
Graphite
ZrO2
MgO
h-BN
Resistive heating
~20 Ohm ~0.03 Ohm
Melting point
(At room pressure)
2715 °C 2852 °C 2973 °C
1-8 mm
1-5 mm
Thermocouple
Type-C
W-5%Re – W-26%Re
(up to 2300 °C)
Type-B Pt-30%Rh – Pt-6%Rh
(up to 1700 °C)

## Slide 49: Beamline characteristics
Schematic overview of the beamline (P61B)
Wigglers (x10)
The last wiggler is
~133m away from the LVP
5 m
9 m